| Buildings Department | Practice Note for Authorized Persons and Registered Structural Engineers | 173 |
| --- | --- | --- |

Safe Design and Construction of

Cantilevered Projecting Structures

Canopies, balconies, bay windows, air-conditioner platforms, windows flower boxes and other similar features are prone to becoming unstable if they are not properly designed, constructed and maintained.  These are features on the exteriors of buildings normally of cantilevered construction projecting from the parent building.  Their collapse would have serious consequences.  This Practice Note gives guidance to Authorized Persons and Registered Structural Engineers on the design and construction of cantilevered projecting structures in the interest of public safety.

Reinforced Concrete Cantilevered Projecting Structures

2.		The most significant aspects relating to the safety of reinforced concrete cantilevered projecting structures are the load carrying capacity of the structural elements and the durability of concrete.  Appendix A gives guidelines on structural design, construction, drainage, site supervision and construction reports for achieving the safety standards.  Appendix B provides recommended details for the arrangement for reinforcements.  Structural submissions not conforming to these recommendations will be considered as not complying fully with the performance requirements set out in Building (Construction) Regulation 4.  The requirements on supervision, standards of workmanship and submission of construction report will be the Building Authority’s pre-requisites for approval of plans and consent to commence works.

|  | ( Marco M H WU ) Building Authority |
| --- | --- |

Ref. : BD GP/BORD/23

First issue  October 1994

Last revision  January 1998

This revision  May 2003 (AD/NB2) – Appendix A revised

Index under :  Cantilevered Projecting Structures

# Appendix A

# (PNAP 173)

Guidance Notes on Design and Construction of

Reinforced Concrete Cantilevered Projecting Structures

Structural Design

1.	For cantilevered projections of span more than 1000 mm., a beam-and-slab type of arrangement should be used instead of pure slab cantilever where practicable. The overall depth of a beam at support should be at least 300 mm.

- In a beam-and-slab type cantilevered projecting structure, the in-fill slabs are not considered as cantilevers and the requirements on the provision of steel reinforcement and their service stress in paragraphs 4 and 6 respectively are not applicable to such slabs.

3.	Where pure cantilever slab projections have to be designed for, the span to overall structural slab thickness ratio should not be greater than 7 and the slab thickness should be adequate to satisfy the structural strength and durability requirements.  If the projecting span exceeds 500 mm, the overall structural slab thickness should not be less than 150 mm.  If the projecting span does not exceed 500 mm, the slab thickness may be reduced but should not be less than 100 mm.  The thickness of the wall supporting the projecting slab should not be less than the thickness of the slab in addition to any other requirement on the design of the wall.

4.	Cantilevered concrete slabs should be reinforced with high yield steel bars in both faces and in both directions.  Main reinforcement bars should be at least 10mm diameter and spacing should not be greater than 150 mm, and the steel area should not be less than 0.25% of the cross-sectional area of the structural concrete.

5.	The main reinforcement of a projecting structure should have adequate anchorage in the supporting member and wherever possible, be rigidly fixed to the reinforcement of the supporting member.  Reinforcement details should be drawn to a large scale indicating clearly the connections.

6.	If a cantilevered projection is exposed to weathering, the service stress for deformed high yield steel and plain mild steel reinforcement used in the design should not exceed 100 N/mm2 and 85 N/mm2 respectively.  Anchorage length should not be less than 45 times the diameter of the steel bar.  The minimum cover to the main reinforcement should not be less than 40 mm.

7.	Consideration should be given to any local reduction in structural strength affected by the surface drainage system or embedded service pipes and ducts.

8.	Allowance should be given to the superimposed loads due to the finishes, waterproofing materials, maintenance work and possible ponding resulting from malfunctioning of the drainage system.

9.	Projections over street could be removed, for various reasons, before the parent building is demolished.  As such removal may affect the structural integrity of the supporting elements of the parent building due to loading redistributions, AP/RSE should therefore make proper provisions in structural design and detailing to allow such projections to be removed without affecting the safety and integrity of the parent building.

Construction

10.	All cantilevered projections should be cast monolithically with and at the same time as the directly supporting members.  Construction joints must not be located along the external edge of the supporting members.  In case this is unavoidable, any alternative construction method must be submitted for prior approval.  Such method should ensure that the finished product would be able to attain a structural strength no less than that provided by monolithic construction, and that it would not invite ingress of water through the joint.

11.	Adequate bar spacers should be provided to maintain the position and alignment of the steel reinforcement.

12.	During concreting, adequate compaction should be given to ensure good quality concrete. Every endeavour should also be made to avoid steel reinforcement from being displaced or depressed.

13.	All props to the soffit formwork for the cantilevered projections should be maintained for at least 14 days.

Drainage for Cantilevered Projecting Structures Exposed to Weathering

14.	Effective waterproofing should be provided on the top surface.

15.	A fall not less than 1:75 should be laid to prevent accumulation of water.

16.	Adequate drainage outlets should be provided.  Where the cantilevered projected structure is not accessible for cleaning/maintenance, the maximum distance between the drainage outlets should be not more than 5 metres.

## Site Supervision

17.	The authorized person/registered structural engineer (AP/RSE) should provide adequate supervision and inspection on the construction of cantilevered projecting structures so as to ensure compliance with the approved plans.

Construction Report for Cantilevered Projecting Structures Exposed to Weathering

18.	For cantilevered projecting structures with a span exceeding 750mm and exposed to weathering, the AP/RSE, in conjunction with the registered general building contractor where appropriate, is required to submit a construction report upon completion of the works.

19.	The construction report should include the following : -

(a)	an as-built plan showing --

(i)	the location and dimensions of the members of the cantilevered projecting structure;

(ii)	the direction and gradient of the fall, where applicable;

(iii)	the location of the drainage outlets/down pipes, where applicable;

(iv)	the thickness of screeding and finishes;

(v)	the location and details of any construction joints for the cantilevered projecting structure;

(vi)	the grade of concrete and steel;

(vii)	the diameter and spacing of steel reinforcement in the cantilevered projecting structure;

(viii)	the date on which the concrete was cast; and

(ix)	the concrete cover of the steel reinforcement at critical positions of cantilevered slabs, as measured by covermeter; and

(b)	record photographs of cantilevered slabs and supporting members showing --

(i)	the condition and arrangement of the fabricated steel reinforcement prior to concreting; and

(ii)	the condition after concreting but before laying of the finishes and waterproofing materials; and

(c)	a certificate in the prescribed form (Form BA 14) confirming that the works have been carried out in accordance with the approved plans and are structurally safe.

(Rev. 5/2003)

For the purpose of this practice note, cantilevered projecting structures shielded by glazing or walls or under cover may be considered as not exposed to weathering.