### Appendix B

(PNAP 248)

Guidelines on Fixing of 4-bar Hinges

4-bar hinges shall be manufactured from stainless steel with adjustable friction shoe, and all stainless steel bars of the hinge shall have a minimum thickness of 2.5mm.  For better corrosion resistance, stainless steel rivets/screws shall be used for the fixing of hinges and aluminium rivets shall not be used as they tend to corrode.  At least 3 Nos. of 4.8mm diameter stainless steel rivets or 5mm diameter stainless steel screws shall be used to fix each bottom and top bars of the hinge to the window frame and the openable sash.

2.		As stainless steel hinges and rivets/screws are used in aluminium window installation, due consideration and measures should be taken to prevent contact between dissimilar metals.

3.		To provide sufficient anchorage for the stainless steel rivet or screw to fasten the hinge to the window frame and the openable sash, a positive mechanical fixing, for example by inserting a stainless steel or hot dip galvanized steel plate or bar/angle of not less than 3mm thick inside the section to provide sufficient threads for the screw(s) shall be adopted.  A typical example of this arrangement is at Annex I.  As an alternative, the window sections for fixing the hinge may be thickened locally to not less than 5mm.  A typical example is at Annex II.  When insertion of an extra piece of stainless steel or hot dip galvanized steel bar/angle inside the section or local thickening to 5mm is not adopted, the thickness of aluminium sections for fixing the 4-bar hinge shall be substantiated by calculations that it could provide sufficient anchorage for the stainless steel rivet or screw.

# Annex I to Appendix B

(PNAP 248)

F

E

D

A, B, C, E, F – LOCATION FOR SCREW TO WINDOW FRAME/SASH

(LOCAL THICKENING BY S.S. PLATE/BAR)

D – LOCATION FOR SCREW TO WINDOW SASH

(LOCAL THICKENING BY ANGLE)

### SECTION X-X

### SIDE HUNG WINDOW WITH S.S. PLATE/BAR AND

ALUMINIUM ANGLE INSERTED FOR FIXING SCREWS

## ELEVATION

S.S. PLATE/BAR

(AT LOCATIONS A, B, C)

# Annex II to Appendix B

(PNAP 248)

5 mm

5 mm

# Appendix C

(PNAP 248)